PMMA

Positive resist

High resolution, poor etch resistance

Commonly used for bi-layer liftoff process

- Spin Resist for 60 seconds

- Bake on hotplate at 170˚C for 15minutes

- Expose at a dose between 800-1200µC/cm2 (can be much higher for thin resist or isolated features)

- Develop in MIBK:IPA 1:3 for 60-75 seconds (for other options see staff)

- Rinse with IPA

- Blow dry with nitrogen

NEB-31A

Negative, chemically amplified resist

Good etch resistance, 30nm minimum resolution

- Spin Resist for 60 seconds

- Bake on hotplate at 110˚C for 2 minutes

- Expose at a dose between 30-60uC/cm2 -can be much higher for thin isolated features

- Post exposure bake on hotplate at 95˚C for 2 minutes

- Develop in MIF 321 for 30 seconds

- Rinse with DI water

- Blow dry with nitrogen

Zep 520a

Positive resist

High resolution, good etch resistance

- Spin Resist for 30 seconds

- Bake on hotplate at 170˚C for 2minutes

- Expose at a dose between 200-300uC/cm2 -can be much higher for thin or isolated features

- Develop in ZED-N50 (n-amyl acetate) for 45 seconds

- Rinse in MIBK for 30 seconds

- Rinse in IPA for 30 seconds

- Blow dry with nitrogen

XR-1541

Negative resist (also a flowable oxide)

High resolution, good etch resistance

Must be stripped with HF or BOE

- Spin Resist for 30 seconds

- Bake on hotplate at 170˚C for 2 minutes (there are many variations of this)

- Expose at a dose between 600-1200uC/cm2 -can be much higher for thin isolated lines

- Develop in MIF 300 for 120 seconds

- Rinse with DI water

- Blow dry with nitrogen

ma-N 2403

Negative resist

Good etch resistance, 50nm minimum resolution

DUV sensitive for mix and match lithography

- Spin Resist for 30 seconds

- Bake on hotplate at 90˚C for 1 minute

- Expose at a dose between 600-1200uC/cm2  (Expose between 350-450 mJ/cm2 for DUV)

- Develop in MIF 300 for 75 seconds

- Rinse with DI water

- Blow dry with nitrogen

Zep 7000-22

Positive, chemically amplified resist

Good etch resistance

High speed makes it ideal for masks and larger features

DUV sensitive for mix and match lithography

- Spin Resist for a minimum of 60 seconds

- Bake on hotplate at 170˚C for 3 minutes

- Expose at a dose between 40-80uC/cm2

- Post Exposure Bake at 115˚C for 2 minutes

- Develop in ZED-500 for 3 minutes

- Rinse in IPA for 30 seconds

- Blow dry with nitrogen